Dongguan Longhai Chemical Co., Ltd

Product Technology Datasheet

204B

Version：22.05.2014

Product Category	Micronized PE wax

Product Feature	The product is a PE wax, its molecular weight distribution is very uniform,  it has the following characteristics

- Low cost

- Improve the smoothness and anti-scratching of the coating film

- Good fineness, narrow particle size distribution

- Low effect on gloss

- Easy to disperse in alcohol/ester oil/liquid oil, good compatibility with resin

Typical Application		The product is recommended to be used in industrial paint, powder coating plus wax, offset printing ink. It is quite high cost-effective.

Usage	This product can be added during any of the processing, it is uniform dispersion after the mixture.

Supplementation Ratio	The recommended supplementation ratio(ratio of the gross ingredient) is 0.5-1.0%, please choose the best supplementation according to the different demands actually.

Technical Specifications	Appearance	                          white powder

Melting point GB/T 12766-2008		118-122℃

Density GB/T 1033.1-2008			0.93~0.95（g/cm3 ）

Penetration value GB/T 4985-2010		＜1.0 （10-1mm）

Average particle diameter GB-T 19077.1-2008		6-8（μm）

Acid value GB264-83                                                  10    （mgKOH/g）

Package and Storage                    The product is packed by 20kg/paper bag, please store it in a cool and  dry place. The storage period of the product is up to 24 months at least, since the delivery date. After it all, the product should be inspected  before usage.

Constitution and  Regulation        All the ingredients are complied with the regulations listed in the TSCA (USA) and the EINECS (EU), and all are safe and environmentally friendly, strictly hew to the latest regulations on environmental protection in Europe. For more information, please feel free to contact us-Longhai Chemical Co., Ltd.

Information and information in this manual is only available as a technical guide to you, and you can refer to it as a technical manual, while the information is not assured and we do not provide any guarantee to it.

The above data only contain the typical technical data of the product, if you need the detailed technical data, you can request our customer service department to offer them.

This version is able to replace the previous version.

"Longhai wax auxiliary agents" is a registered trademark by Longhai Chemical Co., Ltd.