Longhai Chemical Co., Ltd

Product Technology Datasheet

992

Version：30.Aug.2017

Product Category	PTFE wax paste

Product Feature	It has the following characteristics:

- Good transparency property.

- Increase the slipping property and scratch resistance of the coating film.

- Low effect on gloss.

Typical Application		Improve anti-abrasion performance in water-based system.

Usage	This product can be added during any of the processing, it is uniform dispersion after the mixture.

Supplementation Ratio	The recommended supplementation ratio(ratio of the gross ingredient) is 1.0-5.0%, please choose the best supplementation according to the different demands actually.

Technical Specifications	Appearance	     white paste

Effective Section		50%

Density GB/T 1033.1-2008		                           0.90~0.95（g/cm3 ）

Particles size                                                             <7μm

Melting point                                                              320℃

Package and Storage                    The product is packed by  25kg/plastic barrel, please store it in a cool and  dry place. The storage period of the product is up to 12 months at least, since the delivery date. After it all, the product should be inspected  before usage.

Constitution and  Regulation        All the ingredients are complied with the regulations listed in the TSCA (USA) and the EINECS (EU), and all are safe and environmentally friendly, strictly hew to the latest regulations on environmental protection in Europe. For more information, please feel free to contact us-Longhai Chemical Co., Ltd.

Information and information in this manual is only available as a technical guide to you, and you can refer to it as a technical manual, while the information is not assured and we do not provide any guarantee to it.

The above data only contain the typical technical data of the product, if you need the detailed technical data, you can request our customer service department to offer them.

This version is able to replace the previous version.

"Longhai chemical" is a registered trademark by Longhai Chemical Co., Ltd.