Dongguan Longhai Chemical Co., Ltd

Product Technology Datasheet

110

Version：12.16.2015

Product Category	Inorganic dispersant agent

Product Feature	It has the following characteristics:

- This product is copolymer which contains acid groups.

- Good effect on viscosity-decreasing for titanium dioxide

- Good dispersion property to inorganic pigments and fillers

- Increase the solidity content of pigments

- Improve the leveling property, improve the gloss

Typical Application		The product is recommended to be used in solvent-based systems, has dispersion and viscosity properties to titanium dioxide, iron oxide red, medium chrome yellow, silica, aluminum hydroxide, calcium carbonate and multi inorganic pigments/fillers.

Usage	This product can be added during any of the processing, it is uniform dispersion after the mixture. It is better performance after the grinding.

Supplementation Ratio	The recommended supplementation ratio(ratio of the gross aluminum powder) is:

Disperse titanium dioxide                         1-2%

Disperse inorganic pigment/fillers             0.52.0%

Please choose the best supplementation according to the different demands actually.

Technical Specifications	Appearance                      Light yellow transparent liquid

Effective section                                                         98±2%

Density GB/T 1033.1-2008		0.86（g/cm3 ）

Acid value                                                                   10-20(mgKOH/g)

Package and Storage                    The product is packed by 25kg/plastic bag, please store it in a cool and  dry place. The storage period of the product is up to 12 months at least, since the delivery date. After it all, the product should be inspected  before usage.

Constitution and  Regulation        All the ingredients are complied with the regulations listed in the TSCA (USA) and the EINECS (EU), and all are safe and environmentally friendly, strictly hew to the latest regulations on environmental protection in Europe. For more information, please feel free to contact us-Longhai Chemical Co., Ltd.

Information and information in this manual is only available as a technical guide to you, and you can refer to it as a technical manual, while the information is not assured and we do not provide any guarantee to it.

The above data only contain the typical technical data of the product, if you need the detailed technical data, you can request our customer service department to offer them.

This version is able to replace the previous version.

"Longhai wax auxiliary agents" is a registered trademark by Longhai Chemical Co., Ltd.